## Slide 1: MOLCAR WP1
SINTEF and WUT 2023 13th Visiting Warsaw
Notes: Bildet illustrerer:
· bredden i SINTEFs ekspertise, fra havrom til verdensrom.
· hvilke områder og bransjer vi jobber innen for å realisere visjonen Teknologi for et bedre samfunn.
Bildestilen er basert på stikkordene fremtidsrettet, teknologi og norsk natur (naturressurser). SINTEFs visuelle univers er utviklet for SINTEF av Headspin Productions AS.

## Slide 2: WP1
Task 1.1: Material screening of solid oxide ion conducting support materials.
Task 1.2: Novel oxides or carbonates can be dissolved into molten carbonates which can increases the oxide ion conductivity contributions.
Task 1.3: Manufacturing of composite membranes.
Task 1.4: Electrical and electrochemical characterization of new designed membranes.

## Slide 3: Material screening:

## Slide 4: Ba-BNT and LNT
Solid state synthesis

## Slide 5: Ba-BNT

## Slide 6: Sample fabrication

## Slide 7: Testing cell setup

## Slide 8: Impedance study – YSZ reference

## Slide 9: Impedance study – LNT-temperature

## Slide 10: Impedance study – LNT-O2%

## Slide 11: Impedance study – LNT-CO2%

## Slide 12: Impedance study – LNT-discharge

## Slide 13: Power study – LNT-discharge

## Slide 14: Power study – LNT,Ba-BNT comparison

## Slide 15: IV of BNT and LNT samples (larger cells)
BNT
LNT

## Slide 16: Power out put for YSZ reference sample
Chart: Current density, mA/cm2
| 0.85901234567901241 | 0.81382716049382731 | 0.81382716049382731 | 3.3909135802469135 | 6.2392592592592591 | 9.4719012345679019 | 12.342864197530863 | 15.123407407407406 | 17.971753086419753 | 20.797481481481483 | 23.713629629629629 | 26.584592592592589 | 29.794666666666668 | 32.710814814814817 | 35.581777777777781 | 38.520543209876543 | 41.617580246913583 | 44.465925925925923 | 47.359506172839509 | 50.16261728395061 | 53.372641975308646 | 56.356641975308641 | 59.159802469135805 | 62.008148148148152 | 64.811259259259245 | 67.953530864197532 | 70.892296296296294 | 73.785827160493824 | 76.272493827160503 | 79.52775308641975 | 82.421333333333337 | 85.631358024691352 | 88.502320987654329 | 91.350666666666669 | 94.1763950617284 | 97.386469135802471 | 99.827901234567904 | 103.1961975308642 | 105.99935802469136 | 108.89288888888889 | 112.10296296296296 | 114.61219753086419 | 117.41535802469134 | 120.7158024691358 | 123.49634567901235 | 126.45772839506172 | 129.35130864197529 | 132.19965432098766
1.2ml/min/cm2 H2/, 1 ml/min/cm2 N2, 2.6 ml/min/cm2 CO2, 28 ml/min/cm2, T=650 | 0.93615 | 0.88544 | 0.8826 | 3.6249 | 6.5575 | 9.8063 | 12.6008 | 15.2474 | 17.8765 | 20.4294 | 22.9927 | 25.4734 | 28.2126 | 30.5552 | 32.842 | 35.1384 | 37.4933 | 39.588 | 41.6764 | 43.6415 | 45.8151 | 47.7961 | 49.6351 | 51.4668 | 53.1517 | 54.9948 | 56.6642 | 58.1949 | 59.5002 | 61.1091 | 62.4012 | 63.7868 | 64.9607 | 66.1653 | 67.2514 | 68.3556 | 69.051 | 70.0289 | 70.3624 | 70.7477 | 70.9836 | 70.9679 | 70.8015 | 70.4256 | 67.8118 | 61.9643 | 49.9425 | 22.8309
0.9ml/min/cm2 H2/, 1.3 ml/min/cm2 N2, 2.6 ml/min/cm2 CO2, 28 ml/min/cm2, T=650 | 0.85166 | 2.0407 | 5.025 | 7.9663 | 10.6213 | 13.7087 | 16.3512 | 18.8871 | 21.596 | 23.7727 | 26.4375 | 28.7514 | 31.0592 | 33.285 | 35.4187 | 37.665 | 39.6903 | 41.6129 | 43.4516 | 45.479 | 47.2797 | 48.8425 | 50.4065 | 51.8511 | 53.4799 | 54.7679 | 55.9187 | 56.8811 | 57.8873 | 58.5072 | 58.9147 | 59.1958 | 59.0863 | 57.8342 | 52.6442 | 27.4659 | 13.344
1.5ml/min/cm2 H2/, 0.7 ml/min/cm2 N2, 2.6 ml/min/cm2 CO2, 28 ml/min/cm2, T=650 | 0.8101 | 0.92258 | 0.85308 | 0.92756 | 0.92833 | 2.092 | 5.116 | 8.0412 | 10.8996 | 14.0878 | 16.723 | 19.412 | 21.9573 | 24.801 | 27.2951 | 29.7365 | 32.1347 | 34.5351 | 37.1322 | 39.3307 | 41.4392 | 43.5771 | 45.6691 | 47.6689 | 49.9817 | 51.8381 | 53.7776 | 55.546 | 57.2882 | 59.009 | 60.6687 | 62.3125 | 63.9746 | 65.3969 | 67.0415 | 68.2587 | 69.7914 | 71.0405 | 72.2382 | 73.3174 | 74.2454 | 75.1094 | 76.013 | 76.7561 | 77.141 | 77.5727 | 78.2338 | 78.6625 | 79.0938 | 79.3141 | 79.6277 | 79.0851 | 78.7656 | 77.8806 | 76.9585 | 73.3287 | 67.6521 | 60.586 | 45.5702 | 19.8338
0.47ml/min/cm2 H2/, 1.73 ml/min/cm2 N2, 2.63 ml/min/cm2 CO2, 6.17 ml/min/cm2, T=650 | 0.88865 | 2.0291 | 10.3047 | 18.0385 | 24.6031 | 29.4747 | 32.9013 | 31.4809 | 13.6887 | 8.0057 | 5.7422

## Slide 17
Oxides addition for electrolytes
Ba
Ca
Pr

## Slide 18: Measurement data of cell performance for different electrolytes

## Slide 19
Ref.
Ba
Ca
Pr

## Slide 20: IV comparison

## Slide 21: Cross-validation of YSZ supported sample

## Slide 22: Cross-validation of YSZ supported sample

## Slide 23: Durability studies - discharge

## Slide 24: Durability studies -OCV

## Slide 25: Stability of BNT cell

## Slide 26: Summary
Experimental observation of high performance of new solid matrix materials of BNT and LNT can be concluded in a small test cell, but not in larger cell configurations due to potentially gas cross over
Oxides addition to the carbonates show lower performance of the cells but potentially extend the cell life time for reducing the electrode solubility
Tape casting method can effectively make cell components with different chemical compositions
Heavy corrosion of the stainless steel support plates were observed which prevent extended long term stability measurement of the cells and could be improved if better support materials were used